# PRODUCT DATA SHEET

Date:                          14/04/20

Customer:		-

| PRODUCT DETAILS |
| --- |
| Description | NHS Approved Disposable Polythene Aprons |
| Size | 686 x 1170mm |
| Thickness | 16mu |
| Application | Apron |
| Food Grade Materials | Yes |
| High Strength | No |
| Printed | N/A |

| NOMINAL SPECIFICATION AND TOLERANCES |
| --- |
| PARAMETER | SPECIFICATION | TOLERANCE |
| Thickness – Spot | 16mu | + / - 10% |
| Dimensions | 686 x 1170mm | + / - 3% |
| Slip | Medium |  |
| Colour & Opacity | White Tint |  |
| Shrink Classification | Non Shrink |  |
| Polymer Density | 0.921 cu/cm |  |

APPEARANCE

There should be no visible defects such as holes or tears.

PRINT DETAILS / PACKAGING SPECIFICATION / ADDITIONAL INFORMATION

Made from first soured virgin polymer. 100% recyclable. Suitable for an environment handling food stuffs*. 600/box, 84boxes/pallet, 50,400/pallet